|  | Fire Retardent ABS Sheet Technical Specifications. Properties; ISO Test Method; Unit; FR ABS. Density; ISO 1183; G/cm³; 1.24. Izod Impact Strength(notched); ISO 180; J/m; 270. Flexural Strength; ISO 178; Mpa; 60. Tensile Strength; ISO 527; Mpa; 39. Falling dart impact Strength²; ISO 6603-1; J; 59.5. Vicat Softening Temperature; ISO 306A; °C; 100. Heat Deflection Temperature; ISO 75A; °C; 91. Flammability Rating; UL94/ V-0; mm; 1.6. ¹Property evaluations on unpigmented raw material from which this sheet is extruded. ² 4.0mm unpigmented sheet.. Fire Retardent ABS Material Safety Data Sheet. Physical Properties. - Flat sheet - smooth or embossed finishes - Melting point 90°C - Specific gravity 1.05gm/cm³ - Bulk density- 650kg/m³ - Insoluble in water - Percentage volatiles by volume – negligible. Fire & Explosion Data. Auto ignition temperature 500°C Flash point 450°C. Fire and explosion hazards; formation of toxic fumes, hydrogen halides and styrene, acrylonitrile and butadiene rubber in trace quantities . Extinguishing media: water fog, carbon dioxide, dry chemical, Special fire fighting procedures; the material is barely flammable. Ingredients / CAS Number. Pigments (Non hazardous) 4% max, Additives (non hazardous) - 10% max, Antimony Trioxide CAS #001309-64-4 12% max, Acrylonitrile Butadiene Styrene CAS#009003-56-9 60% max, Bis-(tri-bromophenoxy) ethane CAS#037853-59-1 20% max.. Health Effects Data. Effects of inhalation; fumes from thermal decomposition and dust generated from machining may cause temporary breathing difficulties. Effects of ingestion - non toxic. Eye contact; Fumes or dust may cause irritation. Skin contact; hot material may cause burns.. First Aid. First aid for inhalation; remove victim to fresh air, seek medical attention if symptoms persist. First Aid for ingestion; seek medical attention if symptoms develop. First Aid for eye contact- flush eye with water. First Aid for skin contact- cool burns with water, seek medical attention for removal of molten material.. Protective Clothing/ Control Measures. Respiratory protection; Dust masks should be available. Eye protection - use safety glasses. Thermal gloves and protective clothing should be worn. Ventilation requirements - good local and adequate general ventilation should be ensured.. Emergency Procedures. Spillage; lift spillage mechanically.. Waste Disposal. Controlled waste; No. Preferred disposal method – incineration or sanitary landfill, regarding local legal requirements.. Ecological Hazards. Water hazard; no ecological hazard. Land hazard – no hazard.. |
| --- | --- |