| High Impact ABS Technical Specification |  |  |  |
| --- | --- | --- | --- |
| Properties | ISO Test method | Unit | High Impact ABS |
| Density³ | ISO1183 | G/cm³ | 1.05 |
| Izod Impact Strength (notched). | ISO180 | J/m | 390 |
| Flexural Strength | ISO178 | Mpa | 55 |
| Tensile Strength | ISO527 | Mpa | 39 |
| Falling Dart Impact Strength² | ISO 6603-1 | J | 100 |
| Vicat Softening Temperature | ISO306A | °C | 104 |
| Heat Deflection Temperature | ISO75a | °C | 86 |
| Flammability Rating | UL94 | - | HB |
| ¹Property evaluations on injection moulded unpigmented material. ²4.0mm unpigmented extruded sheet ³Density values vary with pigmentation |  |  |  |

High Impact ABS Material Safety Data Sheet

Physical Properties

- Flat sheet - smooth or embossed finishes - Melting point 90°C - Specific gravity 1.05gm/cm³ - Bulk density- 650kg/m³ - Insoluble in water - Percentage volatiles by volume – negligible

Fire & Explosion Data

Flash point –300°C. Extinguishing media – Water fog, foam carbon dioxide dry chemical..

Ingredients

Pigments (non hazardous) 4%max, Additives (non hazardous) 10% max. Acrylonitrile Butadiene Styrene (CAS#009003-56-9) – 90%

Health Effects Data

Effects of inhalation; fumes from thermal decomposition and dust generated from machining may cause temporary breathing difficulties. Effects of ingestion – non toxic. Eye contact; Fumes or dust may cause irritation. Skin contact; hot material may cause burns.

First Aid

First aid for inhalation; remove victim to fresh air, seek medical attention if symptoms persist. First Aid for ingestion; seek medical attention if symptoms develop. First Aid for eye contact- flush eye with water. First Aid for skin contact- cool burns with water, seek medical attention for removal of molten material.

Protective Clothing/ Control Measures

Respiratory protection; Dust masks should be available. Eye protection – use safety glasses. Thermal gloves and protective clothing should be worn. Ventilation requirements – good local and adequate general ventilation should be ensured.

Emergency Procedures

Spillage; lift spillage mechanically.

Waste Disposal

Controlled waste; No. Preferred disposal method – incineration or sanitary landfill, regarding local legal requirements.

Ecological Hazards

Water hazard; no ecological hazard. Land hazard – no hazard.

Transport.

Special requirements- none. Labelling – (not dangerous).