| TYPICAL PROPERTIES of EXTRUDED PEEK |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| ASTM or UL test | Property | Unfilled | 30% Glass Fibers | 30% Carbon Fibers | Bearing Grade |
| PHYSICAL |  |  |  |  |  |
| D792 | Density (lb/in³) (g/cm³) | 0.047 1.31 | 0.056 1.54 | 0.051 1.41 | 0.052 1.44 |
| D570 | Water Absorption, 24 hrs (%) | 0.10 | 0.10 | 0.06 | 0.05 |
| MECHANICAL |  |  |  |  |  |
| D638 | Tensile Strength (psi) | 16,000 | 18,000 | 26,000 | 11,000 |
| D638 | Tensile Modulus (psi) | 500,000 | 1,000,000 | 1,400,000 | 850,000 |
| D638 | Tensile Elongation at Break (%) | 20 | 3 | 1 | 2 |
| D790 | Flexural Strength (psi) | 25,000 | 28,000 | 38,000 | 27,500 |
| D790 | Flexural Modulus (psi) | 600,000 | 1,000,000 | 1,700,000 | 1,100,000 |
| D695 | Compressive Strength (psi) | 20,000 | 26,000 | 29,000 | 26,700 |
| D695 | Compressive Modulus (psi) | 500,000 | 1,000,000 | - | 1,000,000 |
| D785 | Hardness, Rockwell | M100 | M103 | M104 | M85 |
| D256 | IZOD Impact Notched (ft-lb/in) | 1.0 | 1.4 | 1.5 | 0.7 |
| THERMAL |  |  |  |  |  |
| D696 | Coefficient of Linear Thermal Expansion (x 10-5 in./in./°F) | 2.6 | 1.2 | 1.0 | 1.7 |
| D648 | Heat Deflection Temp (°F / °C) at 264 psi | 320 / 160 | 600 / 315 | 550 / 288 | 383 / 195 |
| D3418 | Melting Temp (°F / °C) | 644 / 340 | 644 / 340 | 644 / 340 | - |
| - | Max Operating Temp (°F / °C) | 480 / 249 | 480 / 249 | 500 / 260 | 482 / 250 |
| C177 | Thermal Conductivity (BTU-in/ft²-hr-°F) (x 10-4 cal/cm-sec-°C) | 1.75 6.03 | 2.98 10.3 | 6.4 22.0 | 1.7 5.9 |
| UL94 | Flammability Rating | V-0 | V-0 | V-0 | V-0 |
| ELECTRICAL |  |  |  |  |  |
| D149 | Dielectric Strength (V/mil) short time, 1/8" thick | 480 | 500 | 32 | - |
| D150 | Dielectric Constant at 1 MHz | 3.30 | - | - | - |
| D150 | Dissipation Factor at 1 MHz | 0.003 | - | - | - |
| D257 | Volume Resistivity (ohm-cm) at 50% RH | 4.9 x 1016 | 5 x 1016 | 105 | 103 |

NOTE: The information contained herein are typical values intended for reference and comparison purposes only. They should NOT be used as a basis for design specifications or quality control. Contact us for manufacturers' complete material property datasheets.
All values at 73°F (23°C) unless otherwise noted.

PEEK HT is a trademark of Victrex USA, Inc.