| Technical Information |  |  |
| --- | --- | --- |
| SHEET |  |  |
| Property | Typical Results | Units |
| Cross breaking strength | 130 | MPa |
| Impact strength, notched, Charpy | 11.5 | kj/m² |
| Compressive strength, flatwise | 310 | MPa |
| Compressive strength, edgewise | 200 | MPa |
| Shear strength, flatwise | 90 | MPa |
| Tensile strength | 68 | MPa |
| Youngs modulus | 6.3 | GPa |
| Water Absorption |  |  |
| - 1.6mm thk | 90 | mg |
| - 3mm thk. | 105 | mg |
| - 6mm thk | 130 | mg |
| - 12mm thk. | 160 | mg |
| Electric strength, flatwise in oil at 90°C |  |  |
| - 1.6mm thk | 4.5 | MV/m |
| - 3mm thk. | 2.6 | MV/m |
| - 6mm thk | 2 | MV/m |
| Electric strength, edgewise in oil at 90°C | 12 | kV |
| Insulation resistance after immersion in water | 1X108 | ohms |
| Relative density | 1.36 | - |
| Maximum working temperature** |  |  |
| - continous | 120 | °C |
| - intermittent | 130 | °C |
| Thermal classification | Class E | - |
| Thermal conductivity through laminae | 0.32 | W/(mK) |
| Thermal expansion in plane of laminae | 2.2 | x10-5/K |
| Specific heat | 1.5 | kj(kgK) |
| Round Rods |  |  |
| Property | Typical Result | Units |
| Flexural strenght | 130 | MPa |
| Water Absorption | 3.3 | mg/cm² |
| Insulation resistance after immersion in water | 1x107 | ohms |
| Axial electric strength in oil at 90°C | 4 | kv |
| Relative density | 1.35 | - |
| Test method as BS EN 61212-2 |  |  |
| Round Tubes |  |  |
| Property | Typical Results | Units |
| Axial compressive strength | 170 | MPa |
| Cohesion between layers | 130 | MPa |
| Water absorption | 3.2 | mg/cm² |
| Insulation resistance after immersion in water | 1x107 | ohms |
| Relative density | 1.35 | - |
| Test method as BS EN 61212-2 |  |  |
| Specification |  |  |
| British Standards |  |  |
| Sheet : BS EN 60893 Type PF CC 203 |  |  |
| Round Rod : BS EN 61212-3-3 Type PF CC 42 |  |  |
| Rectangle Bar : BS6128 Part 4 Type PF CC 43 |  |  |
| Hexagon Bar : BS6128 Part 6 Type PF CC 63 |  |  |
| Round Tube : BS EN 61212-3-2 Type PF CC 33 |  |  |
| Rectangular Tube : BS6128 Part 13 Type PF CC 132 |  |  |
| NEMA* |  |  |
| Sheet : LI-1-1983 Type CE |  |  |
| MIL* |  |  |
| Sheet : MIL-I-24768 |  |  |
| DIN* |  |  |
| Round Rod and Tube : DIN7735 Type Hgw 2088 |  |  |